## Slide 1: EUV Lithography
齐争
11/4/2015

## Slide 2: In order to keep pace with the demand for the printing of ever smaller features, lithography tool manufacturers have found it necessary to gradually reduce the wavelength of the light used for imaging and to design imaging systems with ever larger numerical apertures.
The region between the lines shows the wavelength and numerical aperture of cameras simultaneously having a resolution of 100 nm or better and a DOF of 0.5 um or better.
is the wavelength of the radiation used to carry out the imaging, and NA is the numerical aperture of the imaging system (or camera or optics)
Why EUV

## Slide 3: Why 13.5nm
Peak reflectivity of 70% can now be routinely attained for Mo:Si ML’s deposited by magnetron sputtering

## Slide 4: Why 13.5nm
Peak reflectivity of 70% can now be routinely attained for Mo:Si ML’s deposited by magnetron sputtering

## Slide 5: Challenges
Source
Strongly absorbed, vacuum
Reflective optical elements instead of refractive
Multilayer coating to achieve reasonable reflectivity
Mask、photoresist、scanner、process technique
The unprecedented degree of perfection in surface figure and surface finish——fabrication、metrology
…………

## Slide 6: Scheme
Notes: 大概的示意图，用的激光器现在有所变化

## Slide 7: Source

## Slide 8: Source-LPP DPP

## Slide 9: Source-LPP DPP
ASML-NXE:3300B -2014
Notes: Input CO2 laser power ~kw，conversion efficient ~3%, dose control

## Slide 10: Source-LPP DPP
ASML-NXE:3300B -2014
70W MOPA-PP source power demonstrated with good
dose control

## Slide 11: Source—LPP DPP
Notes: debris protection, collector contamination, In-situ collector cleaning

## Slide 12: Source—LPP DPP
Journal of Modern Physics, 2014, 5, 285-295

## Slide 13: Source-FEL
Notes: debris protection, collector contamination, In-situ collector cleaning

## Slide 14: Source-FEL

## Slide 15: Source-FEL
FEL oscillator for EUV lithography(2014)
PhysRevSTAB.14.040702(2011)
Multiturn ERL with FEL— SASE ~5kw

## Slide 16: Source-FEL
Schematic diagram of a FEL designed for self-seeding
Schematic diagram of a regenerative amplifier FEL (RAFEL)
Proc. of SPIE Vol. 9422 94220D-2(2015)
Notes: SASE, self-seeding, regenerative amplifier FEL

## Slide 17: Source-FEL
Proc. of SPIE Vol. 9422 94220D-2(2015)
Comparison of presented FEL operational modes
Notes: SASE, self-seeding, regenerative amplifier FEL

## Slide 18: Source-FEL
Notes: SASE, self-seeding, regenerative amplifier FEL

## Slide 19: Source-FEL
Proc. of SPIE Vol. 9422 94220D-2(2015)
Comparison of energy efficiency options for FEL operation
Notes: SASE, self-seeding, regenerative amplifier FEL

## Slide 20: Source-FEL
Proc. of SPIE Vol. 9422 94220D-2(2015)
FEL operation efficiency options comparison relative to availability
Notes: SASE, self-seeding, regenerative amplifier FEL

## Slide 21: Source-FEL
2014 EUV Workshop on EUV and Soft X-ray Sources

## Slide 22: Source-FEL
2014 EUV Workshop on EUV and Soft X-ray Sources

## Slide 23: Source-FEL
2014 EUV Workshop on EUV and Soft X-ray Sources

## Slide 24: Mask

## Slide 25: Mask

## Slide 26: Photoresist
Resolution
Line-edge roughness
Sensitivity

## Slide 27: Conclusion
FEL-Based EUV sources | 
Pros | Cons
High average power ~kW | Cost (Construction and Operation)
Clean (No debris) | Big footprint
Tunable | Technical complexity
 | Optics damage (high brilliance)
 | Need optimization
Optimization——SASE FEL pulse (typically 0.1mJ, 100fs, 1 mm diameter) high beam fluence (resist ablation threshold), high spatial coherence (speckle and interference patterns), random longitudinal mode spikes of high peak power micro pulses (not favourable to resist chemistry).

## Slide 28
Thank you!